EN 10028-3 P355N steel plate/sheet for Boilers and Pressure Vessels
Key words :
P355N steel plate/sheet, EN 10028-3 P355N steel plate/sheet, EN 10028-3 P355N steel plate/sheet for Boilers and Pressure Vessel steel, P355N steel plate/sheet for Boilers and Pressure Vessel, EN 10028-3 steel plate for Boilers and Pressure Vessel using, P355N steel supplier/Chinese supplier, P355N steel price...

Equivalent grade :
P355N steel plate/sheet is in EN 10028-3 standard. The equal material of P355N steel is: DIN 17102 StE355, UNI7382 FeE355KG, UNE36081 AE355KG, BS1501 223Gr. 490

| P355N EN 10028-3 MATERIAL# 1.0562 | Comparison of steel grades |
| --- | --- |
|  | UNI7382 | FeE355KG |
|  | DIN17102 | StE355 |
|  | UNE36081 | AE355KG |
|  | BS1501 | 223Gr. 490 |

EN 10028-3 P355N steel Chemical Composition % : 
Main chemical composition in EN 10028-3 P355N steel: Carbon Max 0.09, Manganese Max 1.05, Silicon max 0.50, More detailed information, Ni Max 0.90 please refer to the flowing table:

EN 10028-3 P355N steel Chemical Composition %

| Grades | C max | Si max | Mn max | Ni max |
| --- | --- | --- | --- | --- |
| P355N | 0.09 | 0.50 | 1.05 | 0.90 |

EN 10028-3 P355N steel Mechanical Properties  
P355N this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 375- 470 MPa (there is different min strength point at the different thickness.) P355N tensile strength is from 350MPa to 560MPa. (different min strength point at the different thickness.) More detailed information about EN 10028-3 P355N steel Mechanical Properties , please refer to the following table:

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t >16mm | 470 | 560 | 24 | - |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.