EN 10028-3 P355NH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P355NH steel plate/sheet, EN 10028-3 P355NH steel plate/sheet, EN 10028-3 P355NH steel plate/sheet for Boilers and Pressure Vessel steel, P355NH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-3 steel plate for Boilers and Pressure Vessel using, P355NH steel supplier/Chinese supplier, P355NH steel price...

Equivalent grade :
P355NH steel plate/sheet is in EN 10028-3 standard. The equal material of P355NH steel is: DIN 17102 WStE 355, EU113 KG,KW,KT, NFA36201 E355FP

| P355NH EN 10028-2 | Comparison of steel grades |
| --- | --- |
|  | EU 113 | KG,KW,KT |
|  | NBN629 | - |
|  | DIN 17102 | W St E 355 |
|  | NFA36201 | E 355 FP |

EN 10028-3 P355NH steel Chemical Composition % : 
Main chemical composition in EN 10028-3 P355NH steel: Carbon Max 0.18, Manganese from 1.10 to 1.70, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.50, More detailed information, please refer to the flowing table:

EN 10028-3 P355NH steel Chemical Composition %

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P355NH | 0.18 | 0.50 | 1.10-1.70 | 0.025 | 0.015 | 0.012 | 0.020 | 0.300 | 0.30 | 0.08 | 0.50 | 0.05 | 0.03 | 0.10 |

EN 10028-3 P355NH steel Mechanical Properties  
P355NH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 295- 355 MPa (there is different min strength point at the different thickness.) P355NH tensile strength is from 450MPa to 630MPa. (different min strength point at the different thickness.) More detailed information about EN 10028-3 P355NH steel Mechanical Properties , please refer to the following table:

| Grade | Thickness (mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| P355NH | ≤ 16 | 355 | 490 to 630 | 21 |
|  | 16＜t ≤40 | 345 | 490 to 630 | 21 |
|  | 40＜t ≤60 | 335 | 490 to 630 | 21 |
|  | 6＜t ≤100 | 315 | 470 to 610 | 21 |
|  | 100＜t ≤150 | 305 | 460 to 600 | 21 |
|  | 150＜t ≤250 | 295 | 450 to 590 | 21 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.