EN 10028-3 P355NL1 steel plate/sheet for Boilers and Pressure Vessels
Key words :
P355NL1 steel plate/sheet, EN 10028-3 P355NL1 steel plate/sheet, EN 10028-3 P355NL1 steel plate/sheet for Boilers and Pressure Vessel steel, P355NL1 steel plate/sheet for Boilers and Pressure Vessel, EN 10028-3 steel plate for Boilers and Pressure Vessel using, P355NL1 steel supplier/Chinese supplier, P355NL1 steel price...

Equivalent grade :
P355NL1 steel plate/sheet is in EN 10028-3 standard. The equal material of P355NL1 steel is: DIN 17102 TStE 355

| P355NL1 EN 10028-2 | Comparison of steel grades |
| --- | --- |
|  | EU 113 | - |
|  | NBN629 | - |
|  | DIN 17102 | T St E 355 |
|  | NFA36201 | - |

EN 10028-3 P355NL1 steel Chemical Composition % : 
Main chemical composition in EN 10028-3 P355NL1 steel: Carbon Max 0.18, Manganese from 1.10 to 1.70, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.50, More detailed information, please refer to the flowing table:

EN 10028-3 P355NL1 steel Chemical Composition %

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P355NL1 | 0.18 | 0.50 | 1.10-1.70 | 0.025 | 0.015 | 0.012 | 0.020 | 0.300 | 0.30 | 0.08 | 0.50 | 0.05 | 0.03 | 0.10 |

EN 10028-3 P355NL1 steel Mechanical Properties  
P355NL1 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 295- 355 MPa (there is different min strength point at the different thickness.) P355NL1 tensile strength is from 450MPa to 630MPa. (different min strength point at the different thickness.) More detailed information about EN 10028-3 P355NL1 steel Mechanical Properties , please refer to the following table:

| Grade | Thickness (mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| P355NL1 | ≤ 16 | 355 | 490 to 630 | 21 |
|  | 16＜t ≤40 | 345 | 490 to 630 | 21 |
|  | 40＜t ≤60 | 335 | 490 to 630 | 21 |
|  | 6＜t ≤100 | 315 | 470 to 610 | 21 |
|  | 100＜t ≤150 | 305 | 460 to 600 | 21 |
|  | 150＜t ≤250 | 295 | 450 to 590 | 21 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.